NCP1608 EVALUATION BOARD FABRICATION NOTES

PCB Name: NCP1608 Evaluation Board

PCB P/N: NCP1608BOOSTGEVB

PCB Rev.: 1

Date: 07/06/09

NOTES: - UNLESS OTHERWISE SPECIFIED

- Fabricate PCB in accordance with IPC-600, using customer supplied data files.

- Material: Epoxy fiberglass FR4 or equiv., 0.062” +/- 0.007” finished thickness.

- Finished copper thickness to be 1oz. minimum.

- Solder mask over bare copper, bottom side, L.P.I., green in color.

- Solder mask registration +/- 0.003”. All traces adjacent to pads shall be completely covered with solder mask.

- All exposed copper areas to be solder coated.

- Silkscreen both sides using white epoxy ink.

- Hole diameter tolerance is +/- 0.003” after plating.

- Hole location +/- 0.003”. Maximum layer to layer mis-registration shall be 0.003”.

- Finished conductor width shall not vary more than +/- 10% from artwork master.

- Warp and twist of board shall not exceed 0.010” inch per inch.

- All dimensions are in inches. Tolerances: .XX = +/- 0.010”, .XXX = +/- 0.005”.

- Vendors UL approved logo to be located on solder or secondary side of board.

- Drawing is viewed from primary side.

- This is a single layer board.

- Drill size units are thousandths of an inch.

- Do not trim silkscreen which flows over via holes.

- Radius external sharp corners 0.062” (4 Pl.)

- Use Gerber generated data for board outline and cut-outs.

- Pins should be facing the secondary or bottom layer.